| Panduit Raised Panel Label |
| --- |
| This specification is intended to outline the physical and chemical properties of Panduit’s GMH3 material and include the following printable material identifiers: |
| Printable Material Suffixes |  |  |
| APT | A0T | *-30-ES |  |  |  |  |
| A8T | AMT |  |  |  |  |  |
| AST | AUT |  |  |  |  |  |
| AWT |  |  |  |  |  |  |
| PRODUCT SPECIFICATIONS: |
| Description: | Material is RoHS compliant (European Union directive 2002/95/EC). GMH3 consists of a polyester film laminated to a microcellular foam backed high tack adhesive. This material is intended for interior and exterior markings. |
| Print Methods: | This material is recommended for thermal transfer printing. |
| Standard Colors: | White, black, yellow, green, red, silver and orange. *-30-ES is preprinted. |
| Thickness: Recommended Ribbons: | 28 - 34 mils (ASTM D3652) RMR4BL-A, RMR4WH |
| Service Temperature Range: | -40°F to 212°F (-40°C to 100°C) |
| Minimum Application Temperature: | 50°F (10°C) |
| Storage Conditions: | Store at 70°F (21°C) and 50% Relative Humidity. |
| PROPERTIES: | PERFORMANCE: |
| Peel Adhesion to: -Stainless Steel -Smooth ABS -Powdercoated surface -Polycarbonate | 100 oz/in (PSTC-101, 20 min dwell) 150 oz/in (PSTC-101, 24 hour dwell) 100 oz/in (PSTC-101, 20 min dwell) 150 oz/in (PSTC-101, 24 hour dwell) 100 oz/in (PSTC-101, 20 min dwell) 150 oz/in (PSTC-101, 24 hour dwell) Tears (PSTC-101, 20 min dwell) Tears (PSTC-101, 24 hour dwell) |
| Shear Test | 24+ hours (PSTC-107) |
| Tack | 72.0 oz/in (PSTC-16) |
| Samples were thermal transfer printed with RMR4BL-A black resin ribbon and RMR4WH white resin ribbon on the Panduit TDP43M printer. Thermal transfer and preprinted samples were tested as follows: |
| UV Resistance: | 12000 hours* no change observed (ASTM G154) |
| Humidity Resistance: | 1000 hours at 100F(37C) and 95% R.H, no visible change observed *Test conducted in the QUV Weatherometer to assimilate 20 years of expected outdoor exposure under normal conditions. |
| Long Term High Service Temperature: | 1000 hours at 212F(100C), no visible change observed |
| Long Term Low Service Temperature: | 1000 hours at –40F(-40C), no visible change observed |
| Abrasion Resistance: | Taber abraser, CS-10 wheels/500 gm wt/175 cycles, no visible change observed (ASMT D3389). |
| PROPERTIES FOR SOLAR APPLICATION:__________________PERFORMANCE: Short term low temperature exposure: 30 days at -51C, no visible change observed Relative Lightfastness and weatherability: 1000 hours, no change observed (ASTM D3424, Method 4) Tensile Strength: MD: 3725 PSI (ASTM D3759) Elongation: MD: 88% (ASTM D3759) Tack: 9.2N (ASTM D2979) Flammability: 154 seconds (ASTM D1000) Adhesion: 44.7 oz/in (ASTM D3330) |
| CHEMICAL/SOLVENT RESISTANCE: Thermal Transfer Print with Black Ribbon The testing was conducted at room temperature. Samples were thermal transfer printed with RMR4BL-A black resin ribbon on the Panduit TDP43M printer. Separate sets were conditioned for 24 hours before being immersed in the following solvents. Testing consisted of 5 cycles of 10 minute immersions in the specified chemical reagent followed by a 30 minute recovery period. After final immersion, samples were rubbed 10 times with a cotton swab saturated with the test fluid. Visual observations were noted for any smear or loss of legibility. Chemical/Solvent Visual Observation of Print without rub Visual Observation of print with rub Isopropyl alcohol No change No change Methyl Ethyl Ketone No change Loss of print legibility Alcohol mix* No change Loss of print legibility Gasoline No change No change Diesel No change No change Skydrol No change Loss of print legibility Mil 5606 oil No change No change 1,1,1-Trichloroethane No change Loss of print legibility 5% Sodium Hydroxide No change No change 10% Sulfuric acid solution No change No change Deionized water No change No change 10% Salt water solution No change No change n-Hexane No change No change Iso-octane No change No change Ethanol No change Loss of print legibility ASTM#3 oil No change No change Acetone No change Loss of print legibility Bleach No change No change *Alcohol mix is 50% ethanol, 30% methanol, and 20% water by volume. MIL-STD-202G, Method 215K, Solution A, C and D: 3 cycles of three minute immersions in specified fluids followed by toothbrush rub after each immersion. Print remains legible in all three fluids. CHEMICAL/SOLVENT RESISTANCE – Thermal Transfer Print with White Ribbon |
| The testing was conducted at room temperature. Samples were thermal transfer printed with RMR4WH white resin ribbon on the Panduit TDP43M printer. Separate sets were conditioned for 24 hours before being immersed in the following solvents. Testing consisted of 5 cycles of 10 minute immersions in the specified chemical reagent followed by a 30 minute recovery period. After final immersion, samples were rubbed 10 times with a cotton swab saturated with the test fluid. Visual observations were noted for any smear or loss of legibility. |
| Chemical/Solvent | Visual Observation of Print without rub | Visual Observation of print with rub |  |  |
| Isopropyl alcohol | No change | No change |  |  |
| Methyl Ethyl Ketone | Loss of print legibility | Loss of print legibility |  |  |
| Alcohol mix* | No change | Loss of print legibility |  |  |
| Gasoline | No change | Loss of print legibility |  |  |
| Diesel | No change | No change |  |  |
| Skydrol | No change | Loss of print legibility |  |  |
| Mil 5606 oil | No change | No change |  |  |
| 1,1,1-Trichloroethane | No change | Loss of print legibility |  |  |
| 5% Sodium Hydroxide | No change | No change |  |  |
| 10% Sulfuric acid solution | No change | No change |  |  |
| Deionized water | No change | No change |  |  |
| 10% Salt water solution | No change | No change |  |  |
| n-Hexane | No change | No change |  |  |
| Iso-octane | No change | No change |  |  |
| Ethanol | No change | Loss of print legibility |  |  |
| ASTM#3 oil | No change | No change |  |  |
| Acetone | Loss of print legibility | Loss of print legibility |  |  |
| *Alcohol mix is 50% ethanol, 30% methanol, and 20% water by volume. |  |  |
| MIL-STD-202G, Method 215K, Solution A, C and D: 3 cycles of three minute immersions in specified fluids followed by toothbrush rub after each immersion. Print remains legible in solution D but is illegible in solutions A and C. CHEMICAL/SOLVENT RESISTANCE - PREPRINTED: Preprinted samples were tested for chemical/solvent resistance at room temperature. Separate sets were conditioned for 24 hours before being immersed in the following solvents. Testing consisted of 5 cycles of 10 minute immersions in the specified chemical reagent followed by a 30 minute recovery period. After final immersion, samples were rubbed 10 times with a cotton swab saturated with the test fluid. Visual observations were noted for any smear or loss of legibility. Chemical/Solvent Visual Observation of Print without rub Visual Observation of print with rub Isopropyl alcohol No change No change Methyl Ethyl Ketone No change No change Alcohol mix* No change No change Gasoline No change No change Diesel No change No change Skydrol No change No change Mil 5606 oil No change No change 1,1,1-Trichloroethane No change No change 5% Sodium Hydroxide No change No change 10% Sulfuric acid solution No change No change Deionized water No change No change 10% Salt water solution No change No change n-Hexane No change No change Iso-octane No change No change Ethanol No change No change ASTM#3 oil No change No change Acetone No change No change *Alcohol mix is 50% ethanol, 30% methanol, and 20% water by volume. MIL-STD-202G, Method 215K, Solution A, C and D: 3 cycles of three minute immersions in specified fluids followed by toothbrush rub after each immersion. Print remains legible in all three fluids. APPROVALS: UL Recognized: UL 969 File Number: MH14979 CUL Recognized: C22.2 No. 0.15-01 File Number: MH 14979 |

# Text boxes

LIMITED WARRANTY

All Panduit Identification Solution Products (except for Software programs) are warranted to be free from defects in material and workmanship at the time of sale but our obligation under this warranty is limited to replacement of the product proved to be defective within 6 months from the date of sale, or in the case of printers, within 90 days from the date of sale.  This warranty is void if the products or printers are modified, altered or misused in any way.  Use of Panduit printers with any product other than the specified Panduit products for which the printer was designed constitutes misuse.  Before using, the user shall determine the suitability of the product for its intended use and user assumes all risk and liability whatsoever in connection therewith.  The foregoing may not be altered except by an agreement signed by officers or seller and manufacturer.

NEITHER Panduit OR SELLER SHALL BE LIABLE FOR ANY OTHER INJURY, LOSS OR DAMAGE, WHETHER DIRECT OR CONSEQUENTIAL, ARISING OUT OF THE USE OF, OR THE INABILITY TO USE THE PRODUCT OR THE PRINTER.

THIS WARRANTY IS MADE IN LIEU OF AND EXCLUDES ALL OTHER WARRANTIES, EXPRESS OR IMPLIED.  THE IMPLIED WARRANTIES OF MERCHANTABILITY AND FITNESS OF PARTICULAR USE ARE SPECIFICALLY EXCLUDED.

The information contained in this literature is based on our experience to date and is believed to be reliable. It is intended as a guide or use by persons having technical skill at their own discretion and risk. We do not guarantee favorable results or assume any liability in connection with its use. Dimensions contained herein are for reference purposes only.  This publication is not to be taken as a license to operate under, or a recommendation to infringe any existing patents. This supersedes and voids all previous literature, etc.